# 生物质纤维在纸基农用薄膜制备中的应用研究

# 摘    要

随着近代石油工业和塑料工业的发展，塑料地膜也随之发展起来的。世界上众多国家在农业应用塑料地膜栽培技术上都取得了显著的成果，地膜覆盖栽培技术已然成为近代农业的一项不可或缺的技术。

随着地膜覆盖栽培技术的普及，塑料制造的垃圾已经产生了数十亿个。由于塑料垃圾不容易降解，对地球环境造成严重的白色污染。因此，各国正在努力研究生物降解膜来代替传统塑料膜，以解决白色污染导致的严重环境污染问题。在国外，生物降解塑料薄膜的研究始于20世纪70年代中期，国内的研究始于20世纪80年代中期。目前各国的可降解薄膜主要集中在以下几个方面：可降解塑料薄膜;生物降解塑料薄膜;淀粉可生物降解薄膜;光生物降解薄膜。

到目前为止，国内外所研究的可降解植物纤维薄膜仍仅限在实验阶段，尚未见到在地膜覆盖栽培中应用的报道。常用聚乙烯、聚丙烯菌袋由于污染的严峻问题，急需生物质纤维的替代，而生物质基农用膜最需要解决的问题是其使用过程中的抗冲击力问题即干强度，以及湿强度问题。

本研究是利用天然生物质纤维做为主要原料，尝试制作可以用作地膜的高强度可降解薄膜材料。以羧甲基纤维素（CMC）、改性淀粉及聚酰胺环氧氯丙烷树脂（PAE）等为薄膜湿增强剂或粘合剂制备地膜，用以增强材料的干、湿强度，从而满足农用膜在正常生产过程中的强度要求。经传统湿法造纸工艺制备可降解薄膜，用于制备农用地膜。通过比较其厚度、定量、抗张强度。并通过控制实验中的变量分析各项指标的影响因素从而优化工艺，最终选择出制作地膜的最佳工艺。

关键词：生物质；地膜；湿强剂；抗张强度

Abstract

With the development of modern petroleum industry and plastics industry, plastic film has also developed. Many countries in the world have made remarkable achievements in the agricultural application of plastic film cultivation technology, plastic film mulching cultivation technology has become an indispensable technology in modern agriculture.

With the popularization of plastic film mulching cultivation technology, billions of plastic waste have been produced. Because plastic waste is not easy to degrade, it causes serious white pollution to the earth's environment. Therefore, many countries are trying to study biodegradable membranes instead of traditional plastic membranes to solve the serious environmental pollution caused by white pollution. In foreign countries, the research of biodegradable plastic film began in the mid-1970s, and in China, it began in the mid-1980s. At present, biodegradable films in various countries are mainly concentrated in the following aspects: biodegradable plastic films; biodegradable plastic films; starch biodegradable films; photobiodegradable films.

Up to now, the biodegradable plant fiber film studied at home and abroad is still limited to the experimental stage, and there is no report on its application in film mulching cultivation. The common polyethylene and polypropylene bags are badly in need of biomass fibers because of the serious pollution problem. The most important problem to be solved in the use of biomass-based agricultural membrane is the impact resistance, i.e. dry strength and wet strength.

以上内容仅为本文档的试下载部分，为可阅读页数的一半内容。如要下载或阅读全文，请访问：https://d.book118.com/535124031142011112