# 电解法制备高铁酸钾的合成争论

摘要

高铁酸钾具有很强的氧化性、选择性以及环境友好特性。人们觉察高铁酸钾可以作为一种高效、无毒的环境友好型多功能水处理剂；高铁酸钾具有很好的选择 性，还可用于有机合成；此外，高铁酸钾还可以用作高能的“超铁”电池的电极材料。因此，高铁酸钾在以上几个领域具有很好的应用前景。但是高铁酸钾的稳定性差，制备和提纯工艺简单，合成条件苛刻；至今尚未得到公认的成熟的生产工艺。本文主要争论直接电解法制备高铁酸钾。

争论电解法制备高铁酸钾的最正确工艺条件，争论电解质溶液的浓度、温度、电流密度、电解时间等工艺参数对高铁酸钾的产量的影响。提高 NaOH 的浓度可以增加高铁酸钾的产量，当浓度增加到 16mol/L 时，产量会下降。上升温度对高铁酸钾产量的提高格外显著，随温度上升在 30℃消灭高铁酸钾产量最大值，随后产量急剧下降。同样电流密度、电解时间对高铁酸钾产量的影响都是先增大再减小，中间存在一个最大值，分别为 53mA/cm2，6h。

试验说明 ：依据对单因 素试验数据进展正交 试验处理得出 64.2mA/cm2 ， 14mol/LNaOH，30℃，6h 为最正确的工艺参数。

关键词：固体高铁酸钾；电解合成；电流密度

Study on ElectrochemicalProcess Preparation ofPotassium Ferrate<VI〕

# Abstract

The iron(VI> derivation, potassium ferrate(VI>(Fe(VI>> has	properties such as oxidizing	power,selectivity, and	a	non-toxic	by-product	Fe(III>,that	make	potassium ferrate(VI> an environmentally friendly oxidant for several applications. Potassium ferrate has been considered for years to treat with natural waters and wastewaters, because of its

environmental friendly properties and its high efficiency. Fe(VI> is also a selective oxidant for a large number of organic compounds with Fe(III> as a by-product.Fe(VI>therefore has a role in greener technology for organic synthesis.Moreover,Ferrate has also been recently used in a new class of “super -iron”batteries，referred to as super-iron batteries, there use the Fe(VI>/Fe(III> system as anode material.In this paper we reported an electrochemical method generation of ferrate.

Study prepared by electrolysis of potassium ferrate optimum conditions to study the concentration of electrolyte solution, temperature, current density, electrolysis time of processing parameters on the production of potassium ferrate impact. NaOH to raise theconcentration of potassium can increase the output of the high-speed railway, when the increased concentration of 16mol / L, the output willbe dropped. Elevated temperature on the production of potassium ferrate was significantly improved, with the temperature at 30 ℃ Ferrate high production value, followed by sharp decline in production. The same current density, electrolysis time on the high yield of Ferrate arefurther reduced to increase the middle there is a maximum, respectively 53mA/cm2, 6h.

Experiments showthat, single factor experiment based on orthogonal experimental processing data obtained 64.2mA/cm 2, 14mol/LNaOH, 30 ℃, 6h the technical parameters for the best

Keywords ： Potassium	ferrate(VI> ； Electrochemical	Method ； current	density

以上内容仅为本文档的试下载部分，为可阅读页数的一半内容。如要下载或阅读全文，请访问：https://d.book118.com/885131314231011034