# Cordage Institute International Guideline

Cl 2001-04

Fiber Rope Inspection and Retirement Criteria

The Guideline that can Provide Enhanced Fiber Rope Durability 	and Important Information for the Safer Use of Fiber Rope

A Service of the

994 Old Eagle School Road Suite 1019

Wayne,PA  19087-1866

C       Cordage  Institute 2004.All rights reserved.No part of this

standard/guideline may be reproduced or utilized in any way or

by any means (electronic or mechanical)without permission

in writing from the Cordage Institute.

Approved for use.

Cordage Institute,994 Old Eagle School Rd.,Suite 1019

Wayne,PA 19087-1866

Tel:610-971-4854·Fax:610-971-4859

E-mail:info@ropecord.com

.        .

Web:www ropecord com

International  Guideline  Cl  2001-04  Fiber  Rope  Inspection  and  Retirement  Criteria

Guidelines  to  Enhance  Durabilty  and  the  Safer  Use  of  Rope

Cordage Institute

International Guideline

Cl 2001-04 First Edition

FIBER ROPE INSPECTION AND RETIREMENT CRITERIA

Guidelines to enhance durability and the safer use of fiber rope

AWARNING

The use of rope and cordage products has inherent safety risks which are

subject to highly variable conditions and which may change over time.

Compliance with standards and guidelines of the Cordage  Institute  does  not    guarantee  safe  use  under  all  circumstances,and  the  Institute  disclaims  any     responsibility for accidents which  may  occur.If the  user  has  any  questions  or  uncertainties about the proper use of rope or cordage or about safe practices, consult  a  professional  engineer  or  other  qualified  individual.

5.2   Review of Records andHistory 	7

6.11      Axial Compression andKink Bands [K] 	17

6.12       Hockle, Twist, Kink or Corkscrew  [L] 	17

International Guideline Cl 2001-04 Fiber Rope Inspection and Retirement  Criteria

Guidelines to Enhance Durability and the Safer Use of Rope

Table of Contents

1.INTRODUCTION  	1

1.1   Purpose 	1

1.3   Rope Materials and Construction 	 2

1.2   Basis for Inspection and Retirement 	 1

1.4   Thimbles 	 2

1.5   Limitations 	2

1.6   Order of Precedence 	3

2.       REFERENCES AND RELATED PUBLICATIONS 	3

2.1   References 	3

2.2   Related Documents 	 3

3.      TERMINOLOGY 	3

3.1   Terms specific to this document 	3

3.2   Other terms and definitions 	4

4.      INSPECTION AND RETIREMENT PROGRAM 	 5

4.1   General 	 5

4.2   Training 	5

4.3   Log and Record Keeping 	6

4.4    User Established Retirement Criteria 	6

5.   “ USED ROPE INSPECTIONAND EVALUATION 	6

5.1    Introduction 	6

5.3  InspectionProcess 	7

5.4 Destructive Testing 	9

6.      TYPES AND EFFECTS OF DAMAGE 	10

6.1 Introduction [A] 	 10

6.2   Excessive Tension/ Shock Loading  [B] 	10

6.3    Cyclic Tension Wear [C] 	11

6.4   ExternalAbrasion [D] 	12

6.5   Cuting [E]  	 13

6.6   Pulled StrandsandYarns [F] 	13

6.7    Flex Fatigue-  Pulleys, Roliers, Chocks, Fairleads, Blocks [G] 	13

6.8    Spliced Eyes and Other Terminations  [H] 	 14

6.10       Creep (cold flow)[J]  	16

6.9   Knots [] 	16

6.13       Sunlight Degradation [M] 	 18

6.15     Dirt and Grit [O] 	19

6.14      Chemical andHeat Degradation  [N] 	18

7.      DISPOSITION 	19

7.1      Introduction 	19

7.2     Repair 	19

Intemational Guideline Cl 2001-04 FiberRope Inspection and Retirement Criteria

Guidelinesto Enhance Durabiltyand the SaferUse of Rope

7.3      Downgrade 	20

7.4     Retire 	 20

8.     KEYWORDS 	20

Appendices

A                Related Publications

B         Rope Log

Sample Mooring Line Log

Towing Line Log

C         Evaluation Guide

D           lllustrations

Rope Typesand Fittings

Damage llustrations

RopeTypes

Figure 1  Figure 2 Figure 3 Figure 4 Figure 5 Figure 6 Figure 7  Figure 8 Figure 9

List of lllustrations

3 Strand Rope

8 Strand Plaited Rope

12 Strand Rope

Double Braided Rope

Wire Lay Rope

Jacketed Rope

Climbing Rope

Thimbles

Plastic Thimble for Fiber Rope

Damage lllustrations

D-001                Fiber Abrasion - Cyclic Tension

D-002               Fiber Abrasion - Cyclic Tension

D-003              Inter-Stand Abrasion

D-004               Matted Intenal Yarns

D-005               Uniform SurfaceAbrasion

D-006             Extensive Surface Abrasions

D-007              Localized External Abrasion

D-008               Localized External Abrasion

D-009             Localized     Jacket    Wear

D-010              Bumand Melting

D-011               Cutting

D-012               Cut in Jacket- Core Exposed

D-013              Pulled Strandin 8-Strand Rope

D-014               Pulled Strand in Double Braid

D-015              Pulled Strand in New Rope

Rope Safer

Intenational    Guideline    Cl    2001-04    Fiber  Guidelines   to   Enhance   Durability   and   the

Inspection    and Use   of   Rope

Retirement    Criteria

| D-016 | Damage -Running Over Pulley |
| --- | --- |
| D-017 | 3-Strand Splice -properly made |
| D-018 | 3-Strand Splice-poorly made |
| D-019 | Wear in Double Braid Splice |
| D-020 | Tearing in Eye Splice |
| D-021 | Rope with and without Thimble |
| D-022 | Knot in Non-spliceable rope |
| D-023 | Hockle |
| D-024 | Corkscrew due to Twist |
| D-025 | Twist in 12-strand Braid |
| D-026 | UV(sunlight)Degradation |
| D-027 | Dirt and Grit |

International      Guideline      Cl      2001-04       Fiber      Rope      Inspection       and      Retirement      Criteria

Guidelines    to     Enhance     Durability     and    the     Safer     Use     of     Rope

# 1.INTRODUCTION

1.1  Purpose

Careful and frequent inspection of fiber rope,using procedures

contained in this document,reflects prudent safety management

required to protect personnel and property.This Guideline provides

information and procedures to inspect ropes and to establish criteria for evaluation.This document provides inspectors with help to make

reasonable decisions regarding retirement or continued use,including repairing or downgrading.

1.2  Basis for Inspection and Retirement

1.2.1    Fiber ropes are employed in a large variety of applications that

differ greatly in the severity of use.In some applications,ropes

can serve for many years.In more severe applications or

under different conditions,the same rope may degrade rapidly.

Also,ropes of different size,construction or material can show

substantial differences in longevity in the same application.For

each specific fiber rope application the user must establish a

basis for retirement that considers conditions of use,

experience with the application and the degree of risk present. See Section 4.4.

1.2.2   An inspector should always act conservatively when evaluating

a rope and making recommendations for further use.Residual strength in a used rope can only be estimated and destructive   test methods are required to be definitive.The visual or tactile methods described herein can only provide an estimate of rope condition.

1.2.3    Ropes that have been properly selected and used may be kept in service with some wear if inspected and evaluated in

accordance with these guidelines.

1.2.4   This document provides guidance for situations where

extensive usage history,documentation,inspection facilities    and testing laboratories are available;however,this is most    frequently not the case.Less comprehensive inspections are very worthwhile and should be carried out.Actions that are    considered minimal are marked ◆ .

1

International      Guideline      Cl      2001-04       Fiber      Rope      Inspection       and      Retirement      Criteria

Guidelines    to     Enhance     Durability     and    the     Safer     Use     of     Rope

1.3.1       7The ropes covered by these Guidelines are made from

synthetic fibers suitable for use in rope or from natural

(organic)fibers.For descriptions and performance data for

synthetic fibers commonly used in rope refer to Ref.1,Cl 2003 “Fiber Properties” .

1.3.2   Rope constructions include the following:

1.3 Rope Materials and Construction

3 and 4 strand laid rope -Figure 1(3 strand only shown)

·  8-strand plaited -Figure 2

8and  12  strand  single  braid  -Figure  3(12  strand  only shown)

·   Double  braid  -Figure  4

·  WirelayJacketed- FiIngduurestri5al  and  Marine  Ropes  -Figure  6(braided

· jacket construKernmantlectonjaciskewnRoes    -Figure    7(rescue,

climbing,rapelling)

1.3.3   This guideline may apply to ropes of other materials and

constructions;however,the inspector should seek advice from the rope manufacturer or other knowledgeable source

regarding rope types not specifically identified herein.

1.4  Thimbles

1.4.1    Thimbles are an important part of many rope applications.     They are used to protect the eye termination of spliced ropes and grommets and should be inspected if present.Figure 8   and 9 show thimbles which are often used on fiber rope.

1.5 Limitations

1.5.1    This guideline does not cover the selection of rope types and

materials for specific applications,nor does it provide

procedures for safe operation and use.Persons selecting rope

must consider their own experience or consult qualified

persons,rope     standards,manuals,regulations,operating

guidelines or the rope manufacturer for information on

list of reference publications regarding rope use.

selection and use of fiber rope.See Appendix A for a partial

2

International      Guideline      Cl      2001-04       Fiber      Rope      Inspection       and      Retirement      Criteria

Guidelines    to     Enhance     Durabilty     and     the    Safer     Use     of     Rope

1.6 Order of Precedence

1.6.1     In the event of conflict between the information in this guideline  and other guidelines,standards or regulations,the user must    determine the order of precedence.When in doubt consult with appropriate authorities.

2.     REFERENCES AND RELATED PUBLICATIONS

2.1  References

The following Cordage Institute (Cl)and other publications provide

additional information about the properties,testing,care and safe use of fiber ropes:

1. Cl2003: Fiber Properties (Physical,Mechanical and Environmental)for  Cable,Cordage,Rope  and  Twine

2.  Cl 1202:Terminology for  Fiber  Rope

3.  Cl1500: Test Methods for Fiber Ropes.Provides the test methods to determine both the basic and the more

advanced physical properties of fiber ropes.

4. CIB-1.4:Fiber Rope Technical Information Manual

(Cordage Institute).Contains basic information for the selection,application and safe use of rope.

5.  CIE-1: Splicing  Handbook,Second  Edition,Barbara Merry.(Available from the Cordage Institute.)

2.2 Related Documents

See Appendix A for a list of other rope related publications that may be a useful supplement to this guideline.

3..             T‘ERMINOLOGY

3.1 Terms specific to this document.

Qualified person:A person who,by possession of a recognized degree or certificate of professional standing,or who,by extensive knowledge, training,and experience,has successfully demonstrated the ability to     solve or resolve problems relating to the subject matter and work.

3

International  Guideline  Cl  2001-04  Fiber  Rope  Inspection  and  Retirement  Criteria

Guidelines  to  Enhance  Durability  and  the  Safer  Use  of  Rope

Working load limit (WLL):The working load that must not be exceeded for a particular application as established by a regulatory or standards  seting agency.The WLL is calculated by dividing the new rope

minimum break strength by a design factor.Absent any official

publication of a WLL for an application,design factors should be

established by a qualified person.Design factors for rope commonly vary between 5 and 12.

Visual inspection:Examination of the exterior or interior of a rope by visual methods,which may include magnification.

Tactile inspection:Manipulation of the rope by hand or other means to determine hardness and flexibility.

Overloading :Exceeding the WLL by 2 or more times or loading a rope to excess of 50%of its published breaking strength.

Shock loading:A sudden application of force at such a rate of speed

that the rope can be seen to react violently.The dynamic effects can be estimated to be well in excess of the WLL.Arresting a falling weight is    the most common example.

3.2 Other terms and definitions.

Other definitions for terms used in this Guideline may be found in Ref.2, Cl  1202,“Terminology for Fiber Rope” .

4

International      Guideline      Cl      2001-04       Fiber      Rope      Inspection       and      Retirement      Criteria

Guidelines    to     Enhance     Durability     and    the     Safer     Use    of     Rope

4.    INSPECTION AND RETIREMENT PROGRAM

4.1 General

The following sections present the requirements for an effective

inspection and retirement program.

4.1.1     The user is responsible to establish a program for inspection  and retirement that considers conditions of use and degree of risk for the particular application.A program should include:

·Assignment  of  supervisory  responsibility.The  user  should assign an individual responsible for establishing the

program,for training and qualifying inspectors and

preserving records.

· Written procedures

·Training

·Record    keeping

Schedule  for  inspections.

4.1.2   ◆  Ropes that secure or control valuable assets or whose

··Establishment of retirement criteria for each application.

failure would cause serious damage,pollution,or threat to life   warrant more scrutiny than ropes in non-critical use.If a fiber   rope is used in a highly demanding application,with potentially critical risks,the advice of a qualified person should be

obtained when developing the specific inspection and

retirement  program.

4.1.3   The user should continue to revise and refine the program

based on experience.

4.2 Training

4.2.1    ◆  Personnel assigned the responsibility for rope inspections

should be properly trained to recognize rope damage and to  understand the rope inspection procedures and retirement     criteria contained in this guideline.The Cordage Institute can provide information on training resources.

5

International    Guideline    Cl    2001-04     Fiber    Rope     Inspection    and    Retirement     Criteria

Guidelines   to   Enhance    Durability   and   the    Safer   Use   of   Rope

4.3 Log and Record Keeping

4.3.1   An important tool for rope evaluation is a log.This will include

data on the type of rope,time in service and description of

intended use.The details of every inspection should be

entered in the log as to date,location and conclusions.The log should include a regular inspection schedule.Typical logs are  shown in Appendix B.

4.4 User Established Retirement Criteria

The user is responsible for inspecting and making decisions on the

disposition of used rope,based on user established retirement criteria.

Refer to Appendix C and the following key points.

4.4.1   User experience with the applicationshall be considered when

preparing retirement criteria.

4.4.2   Any relevant regulatory standards and guides should be

reviewed and the relevant requirements incorporated into the

program

4.4.3   Examples of sources are:

American National Standards Institute (ANSl)

Occupational Safety and Health Administration (OSHA) Code of Federal Regulations (CFR)

5.     USED ROPE INSPECTION AND EVALUATION

5.1 Introduction

5.1.1   ◆  During the inspection,identify the rope specimen by a

dated tag with separate designation codes for each specimen.

5.1.2   ◆ The inspector determines the disposition of each rope by

comparing results of the evaluation to the user defined retirement criteria.

5.1.3   Complete used rope evaluation includes familiarization with

rope history,visual and tactile inspection,and supplemental     testing if necessary.A general knowledge of the usage history of the rope can aid the inspection process by identifying

potential types or locations of damage.Supplemental testing may be necessary when more quantitative assessments are

6

International      Guideline      Cl      2001-04       Fiber      Rope      Inspection       and      Retirement      Criteria

Guidelines    to     Enhance     Durability     and    the     Safer     Use     of     Rope

required;these may include destructive strength tests,

microscopic examination or chemical analysis.

5.2 Review of Records and History

5.2.1   Ascertain the type and size of the rope and obtain the

specifications for strength if possible.

5.2.2   ◆  Determine the conditions of use by witnessing the

operation or by interviewing personnel.

5.2.3   ◆  Identify and quantify,if possible,unusual events that  may

have damaged the  rope;such as,overloading,impact  loading, long duration of sustained loading,sunlight or chemical

exposure,and  heat  exposure.

5.2.4   Determine the time in service.

5.2.5   ◆  If a rope log is available,examine it for rope identification,

specifications and history.Try to verify that the data matches the specimen.

5.3 Inspection Process

5.3.1   Prepare Inspection Record Sheets or make entries in a log

(refer to Section 4.3).Fill-in known rope information,such as:

type,diameter/circumference,fiber    material,length,

manufacturer,length and type of service.Add name of the inspector,date  and  location.

5.3.2   Photograph the rope if appropriate.

5.3.3   ◆  Lay out the rope in a straight line,on a smooth surface,

underhand tension.Attempt to apply enough tension to

straighten the rope (in increments if space is limited).Small

diameter ropes may be inspected by pulling segments hand-

over-hand.For long lengths of larger ropes,it is best to utilize a

mechanical advantage to apply light tension on the rope while

it is being inspected.

5.3.4   If a rope is long,it may be marked and coded in evenly spaced

intervals.For easier identification,mark each fifth and tenth

length interval more strongly.If the rope is very dirty,intervals   could be marked by using knotted twine pieces passed through the rope.Tape is also appropriate if wrapped completely

around the rope

7

International  Guideline  Cl  2001-04  Fiber  Rope  Inspection  and  Retirement  Criteria

Guidelines  to  Enhance  Durability  and  the  Safer  Use  of  Rope

5.3.5   ◆ Visually examine,stepwise,the entire  rope  length for

detectable damage and deterioration;include eye splices

and/or end-to-end splices [long or short].Record all findings; identify end-to-end location of detectable damage areas.

5.3.6   ◆ Sight the rope down its length as you would a plank or

mast.Inspect for high or low strands and randomly uneven

cross sections.Look for twist in braided and plaited ropes,and corkscrewing in stranded ropes.

5.3.7   ◆  For ropes small enough for a tactile inspection,feel for

unevenness,rough spots and stiff (lacking flexibility)sections.

5.3.8   Measure the rope circumference.Determine the

circumference in a number of places,in particular in any

damaged areas.This is most easily done with a thin whipping twine,thin metal or fabric tape measure or a pi-tape,wrapped around the rope with slight hand tension.Make note of

nominal circumference,and any point on the rope where the     circumference varies more than 10 percent from what is found on most of the rope.Ropes may decrease in circumference if  well used and may be less than specified for new ropes.

5.3.9   Look for variations in the lay length (in a twisted rope)or pick length (in a braided or plaited rope).Apply a small tension to  the rope and check this length at various locations along the  rope.Note any appreciable deviations in lay or pick length.

This length should not vary by more than±5 percent over the rope length.On long specimens,the tension must be high

enough to minimize the effects of friction with the ground

5.3.10  ◆ Examine  the  rope  for  abrasion,cuts,broken  yarns.Make a note of the type,location and level of damage such as,

number of broken or noticeably damaged yarns,depth and

length of abrasion or wear spots,frequency and spacing of

damage,if damage is one strand or multiple strands.Estimate the loss of strength by comparing abraded or cut fibers as a

percentage of the rope diameter or strand diameter.

Lengthwise damage of several adjacent strands should be summed the same as if it were around the circumference.

8

International      Guideline      Cl      2001-04       Fiber      Rope      Inspection       and      Retirement      Criteria

Guidelines    to     Enhance     Durability     and    the     Safer     Use     of     Rope

5.3.11 Check any  broken  rope specimens  in detail.A  meaningful

inspection must include both ends of a broken rope.Note

location and nature of break.If possible,identify the conditions that caused the damage,such as rough hardware surfaces,     points of contact,excessively sharp bends,or introduction of

twist from winching practices.

5.3.12  ◆  Open the rope and examine the interior.Turn twisted rope slightly to open the interior for observation.Push on single

braided or plaited ropes and/or use a fid to open the interior to    view.On double braided ropes,push on the rope and use a fid to open a small hole to view the core.Be careful not to pull

strands excessively.Look for broken filaments,fuzzy areas,

kink bands.

5.3.13  ◆  Check braided ropes for hardness.Pushing on the rope should cause the braids to open.Braided ropes should be    supple and bend easily.They should flatten slightly when     compressed laterally

5.3.14  ◆  Check Kernmantle,jacketed ropes or double braids for core breaks.This is manifested by sudden reduction in

diameter and can be felt by running hands over the rope.

5.4 Destructive Testing

5.4.1   For more definitive estimate of residual strength,a portion of

the rope or its components (yarns or strands)can be removed

and tested for residual strength.For used ropes from the

same or similar applications,periodic destructive testing for

strength and elongation can provide important data for

purposes of evaluation.Samples from the actual rope or its

components can be tested to provide comparative data.

Testing may use the procedures of Ref.3,Cl 1500,“Test

Methods for Fiber Rope".Used rope and rope component

testing and evaluation should be directed by a qualified person.

9

International  Guideline  Cl  2001-04  Fiber  Rope  Inspection  and  Retirement  Criteria

Guidelines  to  Enhance  Durability  and  the  Safer  Use  of  Rope

6.     TYPES AND EFFECTS OF DAMAGE

Appendix C provides evaluation guidance for the various types of  damage.The applicable section letter in this appendix is shown in brackets  []after  the  title.

6.1 Introduction [A]

Knowing the causes and appearance of damage is essential to a good rope inspection and essential in determining retirement criteria.This

section describes the most common causes of rope damage and describes the effects.Appendix D contains pictures or diagrams  illustrating these conditions.

Smaller ropes,due to their reduced bulk,suffer a proportionately larger

loss of strength than larger ropes due to cuts,abrasion,and

environmental exposure.Extra attention is recommended when inspecting small diameter ropes.

6.2 Excessive Tension /Shock Loading [B]

6.2.1   (Overloading or shock loading a rope above a reasonable

working load limit can cause significant loss of strength and/or durability.However,the damage may not be detectable by

visual or tactile inspection.The usage history of a rope is the     best method to determine if excessive tension or shock loading has occurred.Overloading and shock loading are difficult to

define and the inspector must take a conservative approach     when reviewing the history of the rope.Repeated overloading will result in similar damage as that caused by cyclic fatigue as  described in Section 6.3.Shock loading may cause internal     melting of fiber.

10

International      Guideline      Cl      2001-04       Fiber      Rope      Inspection       and      Retirement      Criteria

Guidelines    to     Enhance     Durability     and    the     Safer     Use     of     Rope

6.3 Cyclic Tension Wear [C]

6.3.1   ◆  Ropes that are cycled for long periods of time within a

normal working load range will gradually lose strength.This

loss of strength is accelerated if the rope is unloaded to a slack

condition or near zero tension between load cycles.The

subsequent damage is commonly referred to as fatigue.

Although there are various mechanisms for the breakdown of

synthetic fibers under cyclic tension,the most common is fiber

to fiber abrasion.See Figure D-001 where long term loading

and unloading has caused a breakdown of yarns in the outer

braid of a double braided rope (lower picture).This rope was

also extremely hard due to internal compaction of broken

fibers.Compare to the upper picture of relatively new rope

which was soft and flexible.

6.3.2   ◆ Braided ropes develop many broken filaments at the

crossover points of strands in the braid due to fiber-on-fiber

abrasion.Occasionally,the broken ends of yarns may appear    as if cut square (a magnifying glass may be necessary).These broken filaments give the rope a fuzzy appearance on the

outside and over the entire length that was under load;this can be so extreme as to obscure the underlying braid structure.

Figures D-002 shows extreme examples of braided ropes that exhibit excessive damage from frequent loading and

unloading

6.3.3   ◆  For braided ropes,broken filaments within the rope can   also mat,entangle and/or leave a powdery residue.Extreme internal filament breakage will make the rope very hard,lose  flexibility and be noticeably larger in diameter (with a

subsequent reduction in length);it may be so hard that it is

impossible to pry the rope open to examine the interior

structure.Melted fiber and fusion may be observed in the core rope or between core and cover.See Figure D-003 for

exposing the inside of the structure.

11

International    Guideline    Cl    2001-04    Fiber     Rope    Inspection    and     Retirement    Criteria

Guidelines   to   Enhance    Durability   and   the    Safer   Use   of   Rope

6.3.4   ◆  For 3 strand twisted and 8-strand plaited ropes most of the

wear will occur on the inside of the rope where the strands rub on each other.Broken,matted filaments and a powdery

residue may be observed.Figure D-004 showshow to expose the inside of the structure by pushing on the rope and possibly exposing one strand.For laid ropes,twist the rope in the

opposite direction of the lay.

6.3.5   Wirelay and Kernmatle ropes usually have a non-load bearing

jacket and must be examined under the jacket.Broken

filaments,powdery residue or fusion may be observed if the interior can be examined.

6.4 External Abrasion [D]

6.4.1   ◆  Most external abrasion is localized.Gouges and strips

along one side of the rope are common;these display cut

fibers and are often accompanied by fusion.Damage sufficient to degrade the rope is usually obvious.More uniform abrasion  may be seen in ropes that are used over fixed objects that bear along a considerable portion of its length,Figure D-005.Also,  dragging over a rough surface will show uniform abrasion.

External abrasion can be distinguished from cyclic fatigue

since the interior of the rope will not have damage and the

damage is rarely uniform as seen in Figures D-006,D-007 and

D-008.

6.4.2   ◆ The surface of the rope may be melted and appear black

due to sliding while bent over surfaces when under high tension.See  Figure  D-010.

6.4.3   ◆ Jacketed ropes require inspection of the outer sheath.

The load bearing core should not be exposed.Loose strands that may snag could be a consideration in some cases.

12

International      Guideline      Cl      2001-04      Fiber      Rope       Inspection      and      Retirement      Criteria

Guidelines    to     Enhance     Durabilty     and     the    Safer     Use     of     Rope

6.5  Cutting  [E}

6.5.1    ◆  t is obvious during visual inspection to see where fibers

have been cut sufficiently to degrade a rope.Damage

assessment includes an evaluation of the amount of affected     fiber,and location and orientation of the cut.For multiple cuts,  the space between damaged areas is important.Figure D-011.

6.5.2   For jacketed ropes where the jacket is non-load bearing,a cut

that does not damage the core will probably not affect the

strength.See  Figure  D-012.However,core  deformation  or herniation could occur on subsequent use if the cover is not repaired.Cores can shift relative to the jacket;further

inspection in the vicinity of the jacket should be performed to  ensure integrity of the core.Cuts to jackets may cause other adverse effects such as handling difficulties,inability to slide  through fittings smoothly,and exposing the core to grit.

6.6 Pulled Strands and Yarns [F]

6.6.1

6.6.2

6.7    Flex

6.7.1

◆ Strands and rope yarns can be snagged and pulled out of the rope structure.The level of damage is a function of the

percentage of the rope cross section that has been lost.See Figures D-013,D-014 and D-015.

Pulled strands in braided rope appear as in Figures D-014 and D-015.

Fatigue-Pulleys,Rollers,Chocks,Fairleads,Blocks    [G]

(Constant bending of any type of rope causes internal and

external fiber abrasion.This is frequently caused by running on pulleys.But,other types of flexing such as frequent bending     over a small radius surface,can also cause fatigue damage.    Flexing over fixed surfaces is often accompanied by surface

wear,especially if sliding action is also present.Wear will

appear on the surface of the contact area.The fibers will

become matted on the surface and/or glazed from heat build- up,especially with ropes using polypropylene fibers.Broken

filaments and fusion,as noted under Section 6.2,will be found  inside the rope over the bending zone but not elsewhere in the rope.Figure   D-016.

13

slightly larger (5%-15%)than the rope when there is little or no tension.

International      Guideline      Cl      2001-04      Fiber      Rope       Inspection      and      Retirement      Criteria

Guidelines    to     Enhance     Durability     and    the     Safer     Use     of     Rope

6.8 Spliced Eyes and Other Terminations [H]

6.8.1   ◆  Check for a properly made eye and end-for-end splices;

splices should always be based on manufacturer's instructions, Cordage Institute Guidelines (Cl 2100 through 2102),or

sources such as Reference 5,CIE-1.A long splice for end-for- end is about 80%efficient;consider this when establishing a     WLL.A properly made 3-strand eye splice is shown in Figure    D-017.

6.8.2   ◆  Damage is common at splices.See figures D-018,D-019,

and D-020.This area always needs to be examined closely.     Look for broken strands at the leg junction (See Figure D-12).,  surface wear in the back (apex)of the eye,flattening where the rope bears on pins or bollards,slippage of tucks in stranded or  twisted ropes and displacement of core/cover for braided rope   with buried splices.

6.8.3   ◆ Eye splices used on small pins (less than one to two times

the rope diameter)are likely to have internal and external

damage.See  Figure  D-020.

6.8.4   ◆ Tucks in 3,8 strand and tucks in tuck splices in single

braided may have slipped in the splice.The buried leg in

single and double ropes may have slipped.Freshly exposed fiber in tucks or buried legs will look clean or have a slightly

different appearance where it has pulled out of the body of the rope.See Figure D-018,an example of a poorly made splice.

6.8.5   Lock stitching should be used with bury splices on single

braided rope.Check to see if they are present.They are often found on double braided ropes.In both cases,they should not be broken

6.8.6   Parallel fiber ropes and some parallel strand ropes require a

continuous whipping function.Damage that allows the whipping to come loose can be dangerous.

6.8.7    The◆ folIlowingnspectsfhoulor cre notosionwheacksnoirnspectsharpinegdthimgesblthesat .

◆  Check that the groove in the thimble for the rope is

· indicate weakness or the potential to cut or abrade the rope.

14

Intermational  Guideline  Cl  2001-04  Fiber  Rope  Inspection  and  Retirement  Criteria

Guidelines  to  Enhance  Durability  and  the  Safer  Use  of  Rope

·◆  Check security of thimbles in the eye of a rope.Fiber rope thimbles,Figure 8,have ears that prevent the eye from turning in the thimble or allowing the thimble to fall out.If

wire rope thimbles are used,they should be tight in the eye or lashed to the legs of the eye to prevent turning or falling  out.Adhesives have also been used successfully to secure rope in a thimble

·Figure 9 shows a different approach to fiber rope thimble    design.The round spool and hood eliminate the problems of turning and falling out.

·Fiber  rope thimbles  designed for  nylon,polyester or

polypropylene ropes may not have sufficient strength if used with very high strength fiber ropes.Heavy duty wire rope

thimbles are suitable for these ropes when the fiber rope and wire rope size are the same.If data is available,determine

strength compatibility.

·Thimble rated load must always exceed the WLL for an application.Ideally,if the breaking strength of a thimble is known,it should exceed the rope strength.

· ◆In  some  cases,a  thimble  should  be  used  but  is  not  and excessive wear has occurred in the back of the eye.

Figure D-021,upper,shows the rope eye directly on a

shackle without a thimble.The rope is bent over about the same diameter as the rope itself.This can give adequate   strength when the rope is new or for very few loadings,but wear can be rapid in severe applications.Figure D-021,     lower,shows a wire rope thimble in the same application.

6.8.8   Other Terminations

◆  Mechanical,potted or other types of terminations may be used with fiber ropes if it can be verified that they have been  qualified for the particular service and installed strictly in

accordance with instructions provided by the manufacturer. These must be examined carefully in accordance with the

recommendations of the manufacturer or qualified person.

Always inspect the interface for abrasion where the rope joins

the fitting.

15

Intemational  Guideline  Cl  2001-04  Fiber  Rope  Inspection  and  Retirement  Criteria

Guidelines  to  Enhance  Durabilty  and  the  Safer  Use  of  Rope

6.9   Knots[]

6.9.1   Some ropes are intended to be used with knots;examples are:

rescue,climbing and arborist ropes.These ropes should be inspected for wear in the rope as it enters or exits the knot.    See Figure D-022

6.9.2   ◆  Unless the application is specifically designed to use

knots,they must not be used unless the working load is

reduced by an appropriate amount (base on 50%of published rope strength unless specific contrary data is available).It is    cause for retirement or downgrading if a knot is not called for    and cannot be removed or the rope reveals structural damage due to knotting

6.9.3   ◆  The inspector should endeavor to determine if a knot is

suitable for the application and was properly tied.

6.10   Creep(cold   flow)[J]

6.10.1  Ropes made of materials that creep (Reference 1)will be

measurably longer if loaded continuously for long periods of time.Creep rates depend on the material,time,temperature and load relative to breaking strength.The inspector should  research the loading history of the rope and determine if the  fiber material is subject to significant creep at the operating   conditions.Ropes made of HMPE and polypropylene are     particularly susceptible and nylon is somewhat susceptible.

6.10.2  Ropes that fail due to creep often retain relatively high strength until they are very close to failure;thus the need to check for

operating conditions that may suggest excessive creep.

6.10.3  Creep also reduces the elongation at failure during a strength test.Maintaining relative high stretch before failure is

important in some applications.In most cases,loss of stretch  can only be determined by a destructive test.Strength testing may not reveal the true condition of the rope unless stretch is  also checked and compared to normal values.

16

International      Guideline      Cl      2001-04      Fiber      Rope       Inspection      and      Retirement      Criteria

Guidelines    to     Enhance     Durability     and    the     Safer     Use     of     Rope

6.10.4  Visual inspection for creep is only possible if the rope is cycled at moderate load a few times to set the structure;then gauge   marks are placed on the rope and the length carefully

measured under reference tension before it goes into service. The recorded length is then compared to the used length

measured under the same reference tension.

6.11  Axial Compression and Kink Bands [K]

6.11.1  Ropes that have a braided or extruded jacket over an inner,

load bearing core are subject to axial compression,as

manifested by kink bands.This occurs mostly in ropes with a    very tight jacket.In severe cases,the rope will have bulges in  zones where kinks are concentrated (bulges often repeat at a   uniform cycle length).If the inner core can be inspected,bands of kinked fibers or yarns that have a Z appearance may be

seen.If damage is severe,the filaments at the Z points will be severed as with a knife.If the jacket cannot be opened for

internal inspection,destructive inspection or testing may be the only means of evaluation.

6.11.2   Kink bands can also appear in splices of very high strength,

high modulus ropes.This is an indication that serious damage   could be present.Destructive testing may be the only means of evaluation.

6.12  Hockle,Twist,Kink  or  Corkscrew  [L]

6.12.1  ◆  If a loop is introduced into a 3-strand rope(or other multi-  strand laid rope),it will tend to hockle when tension is applied. Once set,hockles cannot be turned back to restore the rope

structure and this indicates severe damage.See Figure D-023.

6.12.2 ◆  Some ropes will display a corkscrew appearance and musi not be used unless restored to normal appearance.Figure D-

024.

6.12.3  ◆ Braided and plaited ropes should display little or no twist,  and those that do must not be used unless restored to normal

appearance.Figure   D-025

17

International      Guideline      Cl      2001-04       Fiber      Rope      Inspection       and      Retirement      Criteria

Guidelines    to     Enhance     Durability     and    the     Safer     Use    of     Rope

6.13 Sunlight Degradation [M]

6.13.11  ◆  UItra-violet (UV)radiation from direct sunlight will cause    brittle and weak outer rope yarns.UV degradation is difficult to inspect visually.Discoloration and brittleness in the filaments

may be observed in some cases.Strength testing of a few surface fibers or the entire rope is required for a definitive   assessment.Figure   D-026.

6.13.2  The affect on the rope is much less as diameter increases.

Damage to very small ropes can be rapid;ropes over 1 inch in  diameter are much less affected.UV degradation is stronger    in the lower latitudes and will progress with time of exposure.    Non-load-bearing jackets or coatings will protect the core rope. Assessment can be difficult and advice of a qualified person

should besought if there is potential for UV damage.

6.14 Chemical and Heat Degradation [N]

6.14.1  ◆Synthetic fiber materials generally resist chemical attack and heat exposure in normal circumstances but can be

weakened in certain situations.Visual inspection may reveal  discoloration and brittleness of the fibers.Melting,bonding of fibers,(Figure D-019)hardening or stickiness may be

observed.However,these manifestations are not always

present.The inspector should research the exposure history of the rope.

6.14.2  ◆ Nylon  ropes,when wet,can  be seriously degraded  by  long term contamination with rust.This can be detected by the

reddish or brown color.

6.14.3 Fiber ropes stored at even moderately high temperatures for long periods of time can be degraded without any visual

indication of damage.

6.14.4 Refer to Cl 2003 for information on the temperature and chemical resistance of fiber materials.

18

International      Guideline      Cl      2001-04       Fiber      Rope      Inspection       and      Retirement      Criteria

Guidelines    to     Enhance     Durability     and    the     Safer     Use     of     Rope

6.15 Dirt and Grit [O]

6.15.1  ◆  Dirt and grit cause internal fiber abrasion in ropes that are in regular use.Most ropes can be forced open for internal

inspection.A magnifying glass may be helpful for identification

of fine particles.Figure D-027.

6.15.2  ◆  Sea water that has dried and has left a salt deposit can be damaging due to internal abrasion if the rope is used in the dry  condition.

6.15.3  ◆  Oil and grease deposits,of themselves,do  not damage   most rope materials.However,they trap dirt and grit and may make the rope difficult or unpleasant to handle.The inspector needs to assess the effects in the light of the application.

7.     DISPOSITION

7.1 Introduction

It is expected that a rope will be left in normal service if no significant

damage is identified.However,when a rope is considered to be

damaged,in accordance with the inspection and evaluation criteria,a

decision must be made to repair,downgrade or retire the rope based on the results of the inspection.

7.2  Repair

7.2.1   If the rope shows severe damage only in a few concentrated

areas,it may be possible to remove the damaged sections and resplice the rope.After completion of new eye splices or end-   to-end splices,pretension or load cycle to set the splice if

possible.For end-for-end  splices,assume  100%strength  for  a

short splice and 80%for a long splice.

7.2.2   Caution:Splicing of a heavily used rope may be impossble,or

very difficult (double braided nylon rope can be particularly

bad).In such cases,there is often a significant strength loss; consultation with a qualified person may be appropriate.For

jacketed ropes where the core is the strength member,it may   be possible to repair the jacket.Follow manufacturers'or other governing guidelines or directions of a qualified person.

19

International    Guideline    Cl    2001-04     Fiber    Rope     Inspection    and    Retirement     Criteria

Guidelines   to   Enhance    Durability   and   the    Safer   Use   of   Rope

7.3   Downgrade

7.3.1   If a rope is damaged and cannot be repaired,the residual

strength of a rope can only be estimated by the inspector.The

decision to downgrade a rope must be made very

conservatively.

7.3.2   Destructive strength testing of yarns or of a specimen of the

rope can be utilized to estimate residual strength when making the decision to downgrade.Test ropes in accordance with

Cordage Institute Standard Test Method Cl 1500-(current).

7.3.3   Using estimates of the reduced breaking strength of a

degraded rope,the inspector or user must determine a working

load limit (WLL)based on a design factor established by the

user.

7.3.4   The user must make certain that downgraded ropes do not find

their way into the original or other applications that require full

strength.

7.3.5   Downgrading may also apply to ropes that have been repaired

by splicing as used rope splices may have questionable strength.

7.4

Retire

7.4.1

7.4.2

Rope must be retired if it is damaged and cannot otherwise be repaired or a use cannot be found for it in a downgraded

condition.

Retired ropes must be disposed of in accordance with any

applicable regulations and rendered unsuitable for future use.

8.      KEYWORDS

Rope

Rope inspection

Fiber rope

Used rope

Thimbles

20

International Guideline Cl 2001-04 Fiber Rope Inspection and Retirement Criteria

Guidelines to Enhance Durability and the Safer Use of Rope

APPENDIX A

RELATED  DOCUMENTS

The following Cordage Institute(Cl)and other publications provide additional information about the properties,testing,care and safe use of fiber ropes:

1.  ASME B30.9 Sling Standard,Chapter 4 (Synthetic Fiber Rope Slings)  2.  ASTM  D4268(current):Test  Methods for Testing Fiber Rope.Provides the test methods to determine the basic physical properties of fiber ropes.   3.  ASTM  F1740 Standard Guide for Inspection (includes log example)

4.  Cl 1201 (current):Fiber   Ropes:General  Standard.Covers  general characteristics and requirements for all fiber cordage and ropes.

5.  Cl1401 (current):Safe  Use  Guidelines:Appendix  (last  page)to  specific rope specifications issued by the Cordage Institute after 1995 (for instance    Cl1201,cited    above).

6.  Cl Publication List of standards for specific constructions and fibers. 7.  ISO  2307

from the following sources:

Documents listed above and references listed in Section 2.1 can be obtained

1.ASME(American  Society  of  Mechanical  Engineers),345  East  47th

Street.New  York,NY  10017

2.  ASTM(American Society for Testing  Materials),100 Bar Harbor Drive, West  Conshohocken.PA  19428-2959

3.Cordage  Institute,994  Old  Eagle  School  Road,Suite   1019,Wayne,PA

19087-1866;Phone:610-971-4854;Fax:610-971-4859;E-mail:

info@ropecord.com;Web:www.ropecord.com.

21

International    Guideline    Cl    2001-04    Fiber    Rope     Inspection    and    Retirement    Criteria

Guidelines   to   Enhance    Durability   and   the    Safer   Use   of   Rope

APPENDIX B

SAMPLE MOORING LINE LOG

Vessel                               I.D.NUMBER

Size                              Fiber                                Construction                                  Length                      Number Eyes                Size Eyes                  /

Mfg or NSN

Spliced by                                                 Date

Inspection Schedule

HISTORY

Date put in service                          Mooring station

| Date | Inspection or Incident | Comments |
| --- | --- | --- |

22

Intemational  Guideline  Cl  2001-04  Fiber  Rope  Inspection  and  Retirement  Criteria

Guidelines  to  Enhance  Durabilty  and  the  Safer  Use  of  Rope

TOWING LINE LOG

Vessel                               I.D.NUMBER

Size                           Fiber                            Construction

Length_                        Type end fitting		 Mfg or NSN 	  Spliced by_                          Date

Inspection Schedule

HISTORY

Date put in service                          Mooring station

| Date | Inspection or Incident | Comments |
| --- | --- | --- |

23

APPENDIX C

EVALUATION GUIDE

DEFINITIONS

| B-stand =8-stand plaited ropes |  | Damage Description =A brief description of types of damage.See the section reference for a more detailed information |
| --- | --- | --- |
| 3-strand =3 and 4 strand laid ropes |  | Repair -Yes =Repair must be made to justify No recommendation in Retire column.See Section 7.2.Repairs may not be feasible in some cases |
| All braids =8 and 12 strand single braids and double braids |  | Downgrade -Ropes may find use in a less demanding or critica application.This is not recommended,however.See Section 7.3 |
| Jacketed =Jacketed ropes with wire ay,parallel sub-rope,parallel strand or parallel fiber load bearing cores |  | Retire -Yes =Do not use for original application. -Best action =Preferred that rope be downgraded or retired |

A.           INITIAL EVALUATION -GENERAL

| Rope type | Damage Description | Sect. Ref | Fig. Ref | Repair | Downgrade | Retire |
| --- | --- | --- | --- | --- | --- | --- |
| All ropes | Rope displays moderate wear.No history of use no records or no specifications.Time in service unknown.No severe damage.Potential persona njury or material damage exists if rope should break | 5.1.3 5.2 | None | No | Possible | Best action |

以上内容仅为本文档的试下载部分，为可阅读页数的一半内容。如要下载或阅读全文，请访问：https://d.book118.com/995044321311011113